## Slide 1: Shift Bragg Grating for Acousto Optic Sensing: Research Overview
What raises at a fixed 20 m mode, and what does not
Evyatar Rubin
Research Overview
September 13, 2026

## Slide 2: Bottom line
Benchmark: a 20 m mode lengthened to a dB peak; compare .
Changing the teeth trades loss against mode width; cavity and lateral structures do not.
TM radiates sideways: a trench or SiN post row raises by a third; TE does not respond.
Inverse design at fixed width: about 6, in progress, below the lab's overshoot.

## Slide 3: Everything tried, and what it does
direction | pol. | loss | mode width | status
linear apodization | TE, TM | down | up a lot | closed
tanh apodization | TE, TM | down | up | closed
overshoot apodization (lab) | TE, TM | down a lot | by amplitude | reference
innermost tooth shift | TE | down | unchanged | closed
innermost tooth shift | TM | down | up | closed
two tooth inverse design | TE | down | slightly up | closed
wider cavity | TM | down | unchanged | closed
air trench | TM | down | unchanged | closed
SiN post row | TM | down | unchanged | closed
25 tooth inverse design | TM | down a lot | held | in progress

## Slide 4: What does not work
direction | pol. | result
SiN Bragg or crystal walls | TM | loss up
metal mirrors | TM | loss up
retro reflecting post rows | TM | no effect
holes inside the core | TM | resonance lost
Huygens or Kerker scatterers | TM | loss up
a second cavity alongside | TE, TM | power drains
shaped trenches | TM | worse than straight
exotic innermost teeth | TE, TM | no effect
𝜋 shift spread over gaps | TM | loss up
trench or post row | TE | no effect

## Slide 5: at the operating point
Chart: loaded Q (log scale)
| plain, TE | plain, TM | SiN post row, TM | air trench, half depth, TM | SiN post rows, TM | air trench, full depth, TM | lab overshoot, TM | inverse design, TM | lab overshoot, TE (projected)
Q | 12903 | 13930 | 16203 | 16942 | 18093 | 18777 | 35000 | 88868 | 250000
All at a 20 m mode and dB peak, 350 nm SiN core. The TE overshoot bar is projected from its intrinsic , not simulated at dB.

## Slide 6: Details
TE, TE versus TM, TM levers, inverse design

## Slide 7: TE: apodization cuts loss and widens the mode
Linear apodization: loss down, mode much wider. Tanh: same gain, less widening.
A few apodized periods are enough; more add nothing.
The lab's overshoot apodization is stronger by far: only its amplitude sets the mode width.

## Slide 8: TE: shifting the innermost teeth recycles the leak
Shifting the innermost teeth outward cuts loss; the mode width stays.
Light that would leak at the cavity is redirected into the mode; the far field collapses to one lobe.
A two tooth particle swarm design gave the best transmission per width; fabricated devices confirmed the shift range.

## Slide 9: TE versus TM
Same length: TM couples more weakly, so less loss, lower , wider mode.
Same peak transmission: TM is longer and its is about three times higher.
At the operating point the plain gratings tie. TM radiates in the propagation plane, TE upward.

## Slide 10: TM: the teeth behave as in TE, except the shift
Apodization: loss down, mode wider.
A large innermost shift widens the mode with no optimum; TM does not recycle at the cavity.
A wider cavity cuts loss with the mode width unchanged.

## Slide 11: TM: an air trench raises by a third
The trench returns the in plane radiation by total internal reflection; the mode width is unchanged.
A trench stopping at the core top keeps most of the gain in one lithography step.
A deep etch conflicts with the PDMS cover, hence the post rows.

## Slide 12: TM: a row of SiN posts does the trench's job
The row is a weak grating: its period sets the beam angle, .
Aimed at the radiation lobe, sliding the row sets the phase: one phase cancels the lobe, the opposite grows it.
A second row on the other side adds a few percent; a third adds nothing.

## Slide 13: Inverse design: in progress
Adjoint optimization of the 25 innermost teeth per side and the cavity, TM.
Peak transmission is maximized with the mode width and the resonance held fixed.
About 6 the plain grating so far. Next: more free teeth, then a TE run seeded from the overshoot profile.